## Slide 1
Comments on A36 Crack Growth Data
SAE FD&E Fall Meeting
Dan Lingenfelser
11 October 2017
Accurate simulations require accurate inputs
Accurate material properties require appropriate test procedures.

## Slide 2: Compact Tension (CT) Crack Growth Specimen
ASTM E647 allows factor of 5 variation in thickness/width ratio
Previous (2010) A36 testing was on 0.25” thick specimens ESE(T) … Newman et al
Total Life A36 testing used 0.75” thickness CT specimen … Dindinger et al
  Deliberately used thick specimen

## Slide 3: Total Life results compared to A36 results in literature

## Slide 4: Test Specimens
Objective: Confirm & understand difference to support recommendations for possible changes to test standard
Six total compact tension specimens cut from total life A36 bar
  Four specimens are 0.75” thick
  Two specimens are 0.25” thick

## Slide 5: Testing Details
Specimen | Beveled holes | B, mm | w, mm | cn, mm | Pcp, kN (a) | Ncp, cycles | R | Pmax, kN
S1 | No | 18.96 | 76.12 | 22.68 | -24.73 | 25,004 | 0.1 | 12.90
S2 (b) | No | 18.96 | 76.26 | 22.90 | -17.79 | 53,926 | 0.1/0.5 | 8.0/14.90
S3 | Yes (c) | 18.90 | 76.24 | 22.89 | -23.13 | 48,071 | 0.5 | 12.90
S4 | Yes (c) | 19.00 | 76.18 | 22.80 | -23.13 | 50,400 | 0.1 | 9.79
S5 | Yes (c) | 6.26 | 76.23 | 22.99 | -8.90 (d) | 10,004 | 0.1 | 2.22
S6 | Yes (c) | 6.27 | 76.25 | 22.92 | -8.90 | 15,404 | 0.5 | 3.67
(a) Maximum load was -0.45 kN
(b) Non-straight crack front at end of R = 0.1 test; continued test at R = 0.5
(c) Beveled on tensile loading part of pin holes; standard pin holes on compression loading
(d) Inadvertent one cycle of -12.2 kN applied at start of compression pre-cracking
Tested in MSU lab – Jim Newman
Data analysis by Chris Keel – MSU ME student

## Slide 6: From efatigue.com using A36 EN properties
This should be close to Newman 0.25” CT specimen
Nf = 48713 cycles
Specified
Smax or emax = 0 MPa
Smin or emin = -180 MPa
Material Type = steel
σf′ = 1072 MPa
b = -.118
εf′ = 1.086
c = -.599
E = 190538 MPa
2NFL = 1e7
K′ = 894 MPa
n′ = .1656
Su = 700 MPa
Surface Finish Type = none
Kt = 5
Use Fatigue Notch Factor = No
Default
SFL = 160 MPa
kSF = 1.000
Calculated
ΔS or Δe = 180 MPa
Sm or em = -90 MPa
emax = -0.00006 mm/mm
emin = -0.00101 mm/mm
Smax = 0 MPa
Smin = -180 MPa
Δσ = 625 MPa
σmax = 216 MPa
Δε = 0.00682 mm/mm
εmax = -0.00429 mm/mm

## Slide 7: From efatigue.com using A36 EN properties
This should be close to FDE CT specimen
Nf = 145277 cycles
Smax or emax = 60 MPa
Smin or emin = -60 MPa
Material Type = steel
σf′ = 1072 MPa
b = -.118
εf′ = 1.086
c = -.599
E = 190538 MPa
2NFL = 1e7
K′ = 894 MPa
n′ = .1656
Su = 700 MPa
Surface Finish Type = none
Kt = 5
Use Fatigue Notch Factor = No
Default
SFL = 160 MPa
kSF = 1.000
Calculated
ΔS or Δe = 120 MPa
Sm or em = 0 MPa
emax = 0.00031 mm/mm
emin = -0.00031 mm/mm
Smax = 60 MPa
Smin = -60 MPa
Δσ = 509 MPa
σmax = 255 MPa
Δε = 0.00371 mm/mm
εmax = 0.00186 mm/m

## Slide 8: Hysteresis used loops for precracking

## Slide 9: Specimen #1 results – 0.75” thick specimen

## Slide 10
Specimen #S1
Specimen #S3
Specimen #S2
Specimen #S4

## Slide 11: Specimen #2 & #3 results – 0.75” thick specimen – R=0.5

## Slide 12: Specimens #2 & #4 – R = 0.1

## Slide 13: Summary/Discussion topics
Demonstrated ability to match both literature data and FDE data
Appears to be relationship between discoloration (gray area) and growth rate
Slower growth rate on S#4 with lower precracking load and lower applied force range
Is discoloration cause or result?
Plan to review surfaces under SEM to look for clues
Consensus is that FDE dataset is best set to use for this project

## Slide 14: Total Life results compared to A36 results in literature