## Slide 1: Sample Geometry
Investigate through-thickness residual stress at the weld toe & mid-plane, where maximum residual stress occurs.

## Slide 2: Final Residual Stress Results (0 mm from Weld Toe)
Side2
Pass,2,3,4
Side1
Pass1,5,6

## Slide 3: Final Residual Stress Results (2 mm from Weld Toe)
Side2
Pass,2,3,4
Side1
Pass1,5,6

## Slide 4: Residual Stress Correlation Next Steps
Casey Gales
10/11/17

## Slide 5: Non-Correlation Potential Causes
Consideration of plate pre-weld stresses
  Blanchard grinding was done
  Measure ground surface with XRD
  Etch ground surface and re-measure with XRD
Microstructural changes due to high heat input
  Take micrographs of the microstructure of the base metal, HAZ and fusion zone

## Slide 6: Future Steps
Prediction with Dr. Goldak
Need Microstructure images
  Volunteers?
Surface XRD measurement
  Volunteers?
Consider future weld studies
  Temperature of steel at multiple locations
  Strain at multiple locations
  Other info