## Slide 1: Analytical Stress Intensity Factor Solutions for Similar and Dissimilar Spot Welds in Lap-Shear Specimens under Clamped Loading Conditions
Shin-Jang Sung and Jwo Pan
Mechanical Engineering
University of Michigan

## Slide 2: Outline
Introduction
Stress intensity factor solutions from structural stress solutions
Effects of different loading conditions in 2-D
Stress intensity factor solutions for spot welds in lap-shear specimens in 3-D
Conclusions

## Slide 3: Introduction
Automotive sheet components are commonly joined by spot welds such as resistance spot welds and continuous welds such as laser welds.
The fatigue strength of these welds are important to the durability of vehicles.
Lap-shear specimens are most commonly used to evaluate the fracture and fatigue strength of welds.
For high cycle fatigue, accurate stress intensity factor solutions for spot welds in lap-shear specimens are important for correlation to the fatigue lives of the welds in the specimens.

## Slide 4: Introduction
Examples of welds
Friction stir spot welds
Laser welds
(top view)
(side view)
(top view)
(side view)

## Slide 5: Introduction
In this study, the analytical stress intensity factor solutions for spot welds in lap-shear specimens are derived with consideration of
  Different loading conditions
  Different thicknesses and materials of the upper and lower sheets
The corresponding finite element analyses are also conducted to benchmark the analytical solutions.

## Slide 6: K1 and K2 Solutions
In Zhang’s paper, the K1 and K2 solutions can be expressed in terms of four normal structural stresses near the crack tip.
Zhang, S., Stress intensities derived from stresses around a spot weld. International Journal of Fracture. 1999;99(4):239-257
Upper sheet
Lower sheet
outer
Crack
Crack tip
inner
inner
outer

## Slide 7: K1 and K2 Solutions
These K1 and K2 solutions can be used for different materials and thicknesses of the upper and lower sheets.
: bimaterial constant
: modulus ratio
: thickness ratio
: angular quantity (related to material properties and thickness ratio)

## Slide 8: Pinned and Clamped Loading Conditions
Most of lap-shear specimens are tested under clamped loading conditions due to the availability of commercial specimen grips.
Simple forms of the analytical solutions of stress intensity factors are only derived under pinned loading conditions due to its simplicity.
Pinned loading condition
Clamped loading condition
Same axial force
Different deformation modes
Different structural stresses

## Slide 9: Free Body Diagrams of Specimens
Pinned loading condition
Clamped loading condition
MA, MB and V are unknown

## Slide 10: Free Body Diagrams of Welds
Pinned loading condition
Clamped loading condition
Three unknowns:
MD, ME and V
All are known
MB is not equal to ME

## Slide 11: Compatibility Conditions at Welds
Welds DCE is treated as rigid.
Segments AD and BE are treated as two cantilever beams fixed at A and B.
The ends of two cantilever beams AD and BE are connected by the rigid body DCE.
Slope continuity:
Displacement continuity:

## Slide 12: Compatibility Conditions at Welds
Slope continuity for the weld at D and E
Displacement continuity requires that
One equation for the equilibrium condition
Three unknowns: MD, ME and V can be solved by three equations.

## Slide 13: Solutions for MD and ME
Solutions for the bending moments MD and ME at D and E are expressed as
Solution for the shear force V is not listed here.
Corrective terms!
Pinned
Clamped

## Slide 14: Structural Stresses near the Welds
Left crack
Right crack
K1 and K2 values for left and right cracks now can be obtained from the K1 and K2 solutions.

## Slide 15: Finite Element Model
L = 55 mm, tl = tu = 1.5 mm, r = 3.8 mm
Upper sheet: Mg (Eu=45 GPa, νu=0.35) or Steel
Lower sheet: Steel (El=207 GPa, νl=0.3)
Pinned loading condition
Clamped loading condition

## Slide 16: Mesh of the Finite Element Model
Element type: CPE8
Element number: 13,496
Quarter point crack-tip elements with collapsed nodes are used.
upper sheet
lower sheet

## Slide 17: Normalized Stress Intensity Factors
To demonstrate the results, several normalized stress intensity factors are defined.
Pinned loading condition
Clamped loading condition
where
,
,

## Slide 18: Similar Fe/Fe Weld with δ = 1
Analytical | Pinned | Clamped | Change
 | 0.8660 | 0.7767 | -10.31%
 | 1.0000 | 0.9226 | -7.74%
 | 1.3229 | 1.2060 | -8.84%
Analytical | Pinned | Clamped | Change
 | 0.8660 | 0.7767 | -10.31%
 | 1.0000 | 0.9226 | -7.74%
 | 1.3229 | 1.2060 | -8.84%
Clamped | Analytical | Computational | Error
 | 0.7767 | 0.7999 | 2.99%
 | 0.9226 | 0.9287 | 0.66%
 | 1.2060 | 1.2257 | 1.63%
Clamped | Analytical | Computational | Error
 | 0.7767 | 0.7999 | 2.99%
 | 0.9226 | 0.9287 | 0.66%
 | 1.2060 | 1.2257 | 1.63%
Pinned | Analytical | Computational | Error
 | 0.8660 | 0.8656 | -0.05%
 | 1.0000 | 0.9998 | -0.02%
 | 1.3229 | 1.3224 | -0.04%
Pinned | Analytical | Computational | Error
 | 0.8660 | 0.8656 | -0.05%
 | 1.0000 | 0.9998 | -0.02%
 | 1.3229 | 1.3224 | -0.04%

## Slide 19: Dissimilar Mg/Fe Weld with δ = 1
Right crack is the critical one in both cases.
For right cracks, Mode 2 (K2) is dominant.
Pinned | Left |  |  | Right |  | 
 | Analytical | Computational | Error | Analytical | Computational | Error
 | 0.5068 | 0.5077 | 0.18% | 1.0402 | 0.9854 | -5.27%
 | 0.5239 | 0.5225 | -0.27% | 1.4231 | 1.4606 | 2.64%
 | 0.7289 | 0.7285 | -0.05% | 1.7627 | 1.7619 | -0.05%
Pinned | Left |  |  | Right |  | 
 | Analytical | Computational | Error | Analytical | Computational | Error
 | 0.5068 | 0.5077 | 0.18% | 1.0402 | 0.9854 | -5.27%
 | 0.5239 | 0.5225 | -0.27% | 1.4231 | 1.4606 | 2.64%
 | 0.7289 | 0.7285 | -0.05% | 1.7627 | 1.7619 | -0.05%
Clamped | Left |  |  | Right |  | 
 | Analytical | Computational | Error | Analytical | Computational | Error
 | 0.5523 | 0.5652 | 2.34% | 0.7088 | 0.6971 | -1.65%
 | 0.5642 | 0.5668 | 0.46% | 1.1575 | 1.1915 | 2.94%
 | 0.7895 | 0.8004 | 1.38% | 1.3573 | 1.3804 | 1.70%
Clamped | Left |  |  | Right |  | 
 | Analytical | Computational | Error | Analytical | Computational | Error
 | 0.5523 | 0.5652 | 2.34% | 0.7088 | 0.6971 | -1.65%
 | 0.5642 | 0.5668 | 0.46% | 1.1575 | 1.1915 | 2.94%
 | 0.7895 | 0.8004 | 1.38% | 1.3573 | 1.3804 | 1.70%

## Slide 20: Dissimilar Mg/Fe Weld with δ = 1
When the BCs are changed from pinned to clamped, the K2 for the critical right crack will decrease by about 20%.
Analytical | Left |  |  | Right |  | 
 | Pinned | Clamped | Change | Pinned | Clamped | Change
 | 0.5068 | 0.5523 | +8.98% | 1.0402 | 0.7088 | -31.86%
 | 0.5239 | 0.5642 | +7.69% | 1.4231 | 1.1575 | -18.66%
 | 0.7289 | 0.7895 | +8.31% | 1.7627 | 1.3573 | -23.00%
Analytical | Left |  |  | Right |  | 
 | Pinned | Clamped | Change | Pinned | Clamped | Change
 | 0.5068 | 0.5523 | +8.98% | 1.0402 | 0.7088 | -31.86%
 | 0.5239 | 0.5642 | +7.69% | 1.4231 | 1.1575 | -18.66%
 | 0.7289 | 0.7895 | +8.31% | 1.7627 | 1.3573 | -23.00%
Sung, S.-J. and Pan, J., Further investigation of stress intensity factor solutions for similar and dissimilar welds in lap-shear specimens under clamped loading conditions. Engineering Fracture Mechanics. 2016;166:60-81

## Slide 21: Spot Welds in 3-D Lap-Shear Specimens
Generalizing 2-D cases to 3-D cases
Additional geometric parameters: overlap H, width 2b
Pinned loading condition
Clamped loading condition

## Slide 22: Free Body Diagrams of Specimens
Pinned loading condition
Clamped loading condition
Forces and moments at boundaries are the same as those in 2-D cases

## Slide 23: Clamped Conditions in 3-D
Spot weld can be assumed to be rigid.
Region between two surfaces SA and SC are further assumed to be rigid to simplify the problem to 2-D.
Same corrective terms as those for the 2-D case

## Slide 24: Structural Stresses near the Welds in 3-D
Only the pinned loading condition is shown here. The clamped loading condition is already handled by the corrective terms.
To derive structural stresses near the spot weld, we concentrate on the square overlap part of two sheets with the spot weld in the center.
Free body diagram of the overlap part
Two critical points

## Slide 25: Decomposition of Loading
The loading can be decomposed into four loading cases: counter bending, central bending, in-plane shear and tension.
Counter bending
Central bending
In-plane shear
In-plane tension

## Slide 26: Structural Stresses near the Spot Weld for Each Loading Case
All normal structural stresses with θ=0 are positive for the material point marked in red.
Counter bending
Central bending
In-plane shear
In-plane tension

## Slide 27: K1 and K2 Solutions
Normal structural stresses near the spot weld can be obtained as
Left-hand side of the spot weld (Point C)
Right-hand side of the spot weld (Point A)
K1 and K2 values for left and right cracks now can be calculated.

## Slide 28: Finite Element Model
L=77.3 mm, tl=tu=0.65 mm, H=47.1 mm, a=3.2 mm
Three b/a ratios are considered: 4.8, 6.0, 10.8 (b = 15.36mm, 19.2 mm, 34.56 mm)
Only a half of the specimen is modeled
Upper sheet: Mg (Eu=45 GPa, νu=0.35) or Steel
Lower sheet: Steel (El=207 GPa, νl=0.3)

## Slide 29: Mesh of the Finite Element Model
Element type: C3D20
Element number: 29,202, 35,352, 39,678
Quarter point crack-tip elements with collapsed nodes are used
Two kinds of loading conditions are considered

## Slide 30: Normalized Stress Intensity Factors
To demonstrate the results, several normalized stress intensity factors are defined.
Q represents either A (right crack) or C (left crack).
Consider both pinned loading and clamped loading conditions.

## Slide 31: Similar Weld (Fe/Fe)
Analytical results are in agreement with the computational results.
Mode 2 (K2) is dominant (different normalized factors).
Pinned b/a | (%) | (%) | (%)
 | 5.54 | 6.70 | 6.25
 | 1.77 | 4.64 | 3.71
 | -1.44 | 1.65 | 1.18
Pinned b/a |  |  | 
 | 5.54 | 6.70 | 6.25
 | 1.77 | 4.64 | 3.71
 | -1.44 | 1.65 | 1.18
Clamped b/a | (%) | (%) | (%)
 | 1.54 | 10.53 | 7.23
 | -2.37 | 9.09 | 5.63
 | -0.16 | 7.66 | 6.52
Clamped b/a |  |  | 
 | 1.54 | 10.53 | 7.23
 | -2.37 | 9.09 | 5.63
 | -0.16 | 7.66 | 6.52
Differences of the computational and the analytical results:

## Slide 32: Dissimilar Weld (Mg/Fe)
Stress intensity factors are larger for the right crack.

## Slide 33: Dissimilar Weld (Mg/Fe)
Stress intensity factors are larger for the right crack.
Pinned b/a | (%) | (%) | (%)
 | 9.75 | 7.84 | 8.57
 | 4.86 | 5.71 | 5.41
 | -1.29 | 4.45 | 3.00
Pinned b/a |  |  | 
 | 9.75 | 7.84 | 8.57
 | 4.86 | 5.71 | 5.41
 | -1.29 | 4.45 | 3.00
Clamped b/a | (%) | (%) | (%)
 | -1.15 | 12.25 | 8.32
 | -7.70 | 10.24 | 5.71
 | -19.79 | 8.73 | 4.68
Clamped b/a |  |  | 
 | -1.15 | 12.25 | 8.32
 | -7.70 | 10.24 | 5.71
 | -19.79 | 8.73 | 4.68
Differences of the computational and the analytical results for Point A:
Sung, S.-J., Chen, J. and Pan, J., Stress intensity factor solutions for similar and dissimilar spot welds in lap-shear specimens under clamped loading conditions. Engineering Fracture Mechanics. 2017;179:328-347

## Slide 34: Conclusions
The analytical and computational K1 and K2 solutions for spot welds in lap-shear specimens are in agreement with each other.
The clamped loading reduces the stress intensity factor solutions for the given specimen geometries by up to 7% for similar spot welds and by about 20% for dissimilar magnesium/steel spot welds.
The fatigue lives of spot welds in lap-shear specimens under clamped loading conditions are higher than those under pinned loading conditions, especially for dissimilar materials with smaller modulus ratios (larger difference in moduli).

## Slide 35: Acknowledgement
The initial support of this research by the U.S. Department of Energy is appreciated.
Helpful discussion of this work with Dr. Shicheng Zhang of Daimler AG is greatly appreciated.

## Slide 36: Appendix

## Slide 37: Revisiting Structural Stresses near the Spot Weld for Each Loading
All normal structural stresses with θ=0 are positive for the material point marked in red.
Counter bending
Central bending
In-plane shear
In-plane tension

## Slide 38: Accurate Structural Stresses near the Spot Weld for Each Loading Case
Counter bending
Central bending
In-plane shear
In-plane tension
where

## Slide 39: Similar Weld (Fe/Fe)
Differences of the computational and the analytical results
Pinned b/a | (%) | (%) | (%)
 | 5.54 | 6.70 | 6.25
 | 1.77 | 4.64 | 3.71
 | -1.44 | 1.65 | 1.18
Pinned b/a |  |  | 
 | 5.54 | 6.70 | 6.25
 | 1.77 | 4.64 | 3.71
 | -1.44 | 1.65 | 1.18
Clamped b/a | (%) | (%) | (%)
 | 1.54 | 10.53 | 7.23
 | -2.37 | 9.09 | 5.63
 | -0.16 | 7.66 | 6.52
Clamped b/a |  |  | 
 | 1.54 | 10.53 | 7.23
 | -2.37 | 9.09 | 5.63
 | -0.16 | 7.66 | 6.52
Pinned b/a | (%) | (%) | (%)
 | 1.29 | 4.92 | 3.49
 | -1.04 | 3.51 | 2.02
 | -2.36 | 1.32 | 0.74
Pinned b/a |  |  | 
 | 1.29 | 4.92 | 3.49
 | -1.04 | 3.51 | 2.02
 | -2.36 | 1.32 | 0.74
Clamped b/a | (%) | (%) | (%)
 | -2.55 | 8.57 | 4.40
 | -5.06 | 7.85 | 3.88
 | -1.09 | 7.28 | 6.05
Clamped b/a |  |  | 
 | -2.55 | 8.57 | 4.40
 | -5.06 | 7.85 | 3.88
 | -1.09 | 7.28 | 6.05
New structural stress solutions
Original structural stress solutions in this presentation

## Slide 40: Dissimilar Weld (Mg/Fe)
Differences of the computational and the analytical results for Point A
Pinned b/a | (%) | (%) | (%)
 | 9.75 | 7.84 | 8.57
 | 4.86 | 5.71 | 5.41
 | -1.29 | 4.45 | 3.00
Pinned b/a |  |  | 
 | 9.75 | 7.84 | 8.57
 | 4.86 | 5.71 | 5.41
 | -1.29 | 4.45 | 3.00
Clamped b/a | (%) | (%) | (%)
 | -1.15 | 12.25 | 8.32
 | -7.70 | 10.24 | 5.71
 | -19.79 | 8.73 | 4.68
Clamped b/a |  |  | 
 | -1.15 | 12.25 | 8.32
 | -7.70 | 10.24 | 5.71
 | -19.79 | 8.73 | 4.68
Pinned b/a | (%) | (%) | (%)
 | 6.11 | 5.52 | 5.75
 | 2.58 | 4.19 | 3.63
 | -1.88 | 3.99 | 2.50
Pinned b/a |  |  | 
 | 6.11 | 5.52 | 5.75
 | 2.58 | 4.19 | 3.63
 | -1.88 | 3.99 | 2.50
Clamped b/a | (%) | (%) | (%)
 | -4.90 | 10.03 | 5.56
 | -10.02 | 8.77 | 3.97
 | -20.37 | 8.27 | 4.18
Clamped b/a |  |  | 
 | -4.90 | 10.03 | 5.56
 | -10.02 | 8.77 | 3.97
 | -20.37 | 8.27 | 4.18
New structural stress solutions
Original structural stress solutions in this presentation
Sung, S.-J. and Pan, J., Accurate analytical structural stress and stress intensity factor solutions for similar and dissimilar spot welds in lap-shear specimens. Engineering Fracture Mechanics. 2017;182:265-286

## Slide 41: Backup

## Slide 42: K for Interface Crack between Two Layers of Dissimilar Materials
(Rice, JAM, 1988)

## Slide 43: Global K for Main Cracks and Local k for Kinked Cracks
The local k solutions are scaled by the global K solutions either by the analytical solutions or finite element analyses.
Cotterell and Rice, IJF, 1980