## Slide 1
Summary of Fatigue Life Testing and
Analysis of the A36 T-Joint Specimens
Machined and Welded
Completed Todate
SAE FD&E Semi-Annual Meeting
Contributors: See Next Slide
11 October 2017
Total Fatigue Life: Crack Initiation and Crack Propagation

## Slide 2: Society of Automotive Engineering Fatigue Design and Evaluation Committee (SAE FD&E) A36 T-Joint Effort Participants/Contributors
SAE FD&E Committee Administrative/Leadership: Chad Kerestes (Previous Chairman)-CAT, Casey Gales (Chairman)-JD, James Patterson (Vice Chairman)-Hendrickson
Machined & Welded T-Joint Component Fatigue Tests: Ryan Blodig, Eric Norton, Mike Lister, and others-JD; Tom Cordes, Dan Lingenfelser-nCode
T-Joint Component Finite Element Analysis: Hayley Brown-CAT, Peter Huffman-JD, Matt Campbell-Kansas State
Generate Strain-life & Crack Growth Data/Strain Measurements: Phil Dindinger - Element Materials Technology; Jonathan Pickworth – Trilion Quality Systems
Residual Stress Distribution Measurements: Perry Mason, Doug Hornbach and Paul Prevey - Lambda Technologies; Adrian DeWald-Hill Engineering
Striation (Marker Band) Measurements: N. Jayaraman, Doug Hornbach and Paul Prevey - Lambda Technologies; Stephen Horstemeyer, Nima Shamsaei,-Mississippi State
Welded T-joint Component Fabrication & Test Direction/Support: Eric Johnson-JD.
Providing the Steel for the Preceding Contributions: Mary Wickham-CAT
Funding for Some of the Preceding Contributions: Steve Haeg-MTS and Brian Dabell-nCode
T-Joint Component Fatigue Life Predictions and Correlation to Test Data: Al Conle-University of Windsor; Semyon Mikheevskiy, Sergey Bogdanov and Grzegorz Glinka-University of Waterloo; Tom Cordes, Andrew Halfpenny-nCode
Residual Stress Subcommittee: Casey Gales (Subcommittee Chairman), Eric Norton, Vipul Shinde, Rakesh Goyal-JD; David Griffith, Justin Mach, Chad Kerestes, Lingyun Pan, William Ulrich, Hayley Brown, Narendra Singh, Randy Peck, Timothy Vik-CAT; Matthew Campbell-Kansas State; Steve Haeg-MTS, John Goldack-Carleton University, Stephanie Swanson-Hendrickson
Welded T-joint Component (2nd Round of Welded Components) Fabrication and Test Direction/Support: Eric Norton, Brandon Evans, and Casey Gales-JD.
And any other participants and contributors: who may have been inadvertently overlooked in the preceding list.
“By participating in organized efforts the committee provides a forum within which members can work together in a synergistic manner to advance the state of the art in structural durability.”
From: Multiaxial Fatigue of an Induction Hardened Shaft (AE28) - Editors: Tom Cordes and Kevin Lease
“Through the years, members have found that the more they participate in the Committee activities, the more they grow in the area(s) of their particular involvement.”
SAE FD&E
1
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Impressed with the amount of group engagement
We all walk away from these meetings learning something

## Slide 3: Total Fatigue Life: Crack Initiation and Crack Propagation
Geometry?
Loading ???
Mat’l Prop??
Stress/Strain Analysis
Fatigue Damage
Unknown Fatigue Life
1) Real World Engineering Problems
Geometry!
Loading!
Mat’l Prop!
Stress/Strain Analysis
Fatigue Damage??
Known Fatigue Life From Fatigue Tests
2) SAE FD&E “T-Bar” Test/Analysis Effort
High Confidence Inputs/Analysis!(!)
Legend
Define Improved Practice??
This effort is using “very well defined/controlled analysis inputs” to address an engineering problem to validate (or not) a potential “Total Fatigue Life Prediction Improved Practice”
Notes: Real World Vs. Defined Experiments

## Slide 4: Machined Specimen Configuration and Test Fixture/FEM Boundary Conditions
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Eliminate the weld entirely – machine the entire specimen from the 101.6 mm x 101.6 mm bar. Duplicate, by machining, the weld profile and weld toe radius as closely as possible so the sample is consistently made from the same material. Comparing the test /analysis from these samples relative to the test/analysis results from the welded samples, will confirm (or not) assumptions like “can we use the base material properties when analyzing welded structures”, etc.
Notes: Welded Vs. Machined
Reduce variables of weld and using base material properties

## Slide 5: Welded and Machined Specimens
Machined T-Bar Replicates
Welded Specimen Geometry
October 11, 2017
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Show photo of machined samples and welded samples
Compare Geometries

## Slide 6: T-Weld Test & Analysis Overview
Test Log
Test Set Up
Specimen Photos / Loading Histories
RPC Iterations / Variable Amplitude Load History Files
Fatigue Life Analysis
Questions / Comments
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Overview

## Slide 7: Test Log – Machined Specimens, Constant, Block, & Variable Amplitude Loading
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Show Log of test results Load level, R-Ratio, Cycles
Excel table with just important info – spec #, max load, r=ratio, block loading (check Tom’s spreadsheet) summary sheet, show striations at two locations on VA

## Slide 8: Test Log – Welded Specimens, Constant, Block, & Variable Amplitude Loading
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Show Log of test results Load level, R-Ratio, Cycles
Excel table with just important info – spec #, max load, r=ratio, block loading (check Tom’s spreadsheet) summary sheet, show striations at two locations on VA

## Slide 9: T-Weld Test Set Up
MTS FlexTest IIm Controller
  Load Control
  Running tests at 5.1 Hz
MTS 793 Series Software
  Basic Testware (constant amplitude)
  MultiPurpose Testware (block loading)
  RPC Pro (variable amplitude loading TBS)
MTS 244 Series Hydraulic Actuator
  11 Kip (50 kN) x 6” (152 mm) stroke
  252.25 Series dual stage servo valve
  MTS Load cell and LVDT
SOMAT eDAQ Lite
  Record time history file
  Collecting Load & Displacement
  Collect strain on certain specimens
Dino-Lite USB Cameras / Laptop
  Capture time-lapse video at weld toe
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Explain typical loading of specimens
Highest tensile residual stress facing away from the actuator

## Slide 10: SAE FD&E T-Weld Test Set Up
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Notes: Show photo of machined samples and welded samples

## Slide 11
222.25mm From Applied Load Line to Radius
Total Fatigue Life: Crack Initiation and Crack Propagation…Info
Specimen in Test Fixture/ for FEM Boundary Conditions

## Slide 12: Machined T-Weld Specimens
24 kN, R= 0.3
24 kN, R= 0.1
18 kN, R= 0.1
10.8 kN, R= -1
24 kN, Variable Amplitude, Block Loading
24 kN (Max/Min), Variable Amplitude,
Time History File (Tx3, Bx1, Sx2)
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results
Notes: Photos of crack surfaces
Constant amplitude vs. variable amplitude
24kN r=0.3, 24kN r=0.1, 18 r=.1 on one slide
totally reversed on one slide
block loading,
VA loading on one slide

## Slide 13
Highest Mean Load -
Crack Has Not Reached Free End
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 14
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 15
Lowest Mean Load -
Crack Has Reached Free End
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 16
Marker Bands
(Blocks of Striations at a Load Level)
5,000 Cycles
24 kN, R= 0.1
40,000 Cycles
24 kN, R= 0.5
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 17
Marker Bands
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 18
Marker Bands
Side of First Cycle In Tension
Side of First Cycle In Compression
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results

## Slide 19
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Results
Notes: Stephen Horstemeyer, Mississippi St. - Fracture Surface Readings

## Slide 20: RPC Iterations
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Procedure
The variable amplitude load histories were created with RPC Pro through an iteration process.
When iterating a test, the goal is to match the signal response to the signal command
For this testing SAE used the transmission, bracket, and suspension load histories that were used in previous SAE fatigue experiments (SAE AE-6, 1977)
Load histories were developed for the total life project individually then concatenated together for a complete variable amplitude time history
Simplified Process –
Create edt (real or edited time history)
Generate desired display (filtered edt)
Iterate the time history until the feedback signal (response) matches the command signal (desired display)
Notes: Talk about iterations / slides with comparable data
Steps
Data
Original data was excel peak-valley TH w/data points in domain (reversals)
nCode
Scaled TH to 24 kN, padded beginning and end of file with zeros to set up start/stop load
Up-sampled files @ 20.48 Hz (Interpolated, Half-sine) so they could be iterated in RPC
Exported into RPC Format
In RPC
Used Header mod tool to change sample rate to 204.8 Hz to compress file for 5 Hz test frequency
Modified ramp points (parabola point manipulation) at beginning and end of file to reduce overshoot at start and end of drive

## Slide 21: RPC Iterations – Transmission Time History
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Procedure
Transmission load history
mean is primarily tensile
8 Iterations
Red – edt
Blue – des display
Green – rsp

## Slide 22: RPC Iterations – Bracket Time History
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Procedure
Bracket load history
mean is primarily around zero
6 Iterations
Red – edt
Blue – des display
Green – rsp

## Slide 23: RPC Iterations – Suspension Time History
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Procedure
Suspension load history
mean is primarily compressive
7 Iterations
Red – edt
Blue – des display
Green – rsp

## Slide 24: RPC Iterations – Final Drive
Complete Drive File –
3 Repeats of Transmission, 1 Repeat of Bracket, 2 Repeats of Suspension
Total Fatigue Life: Crack Initiation and Crack Propagation…Test Procedure
Notes: Talk about iterations / slides with comparable data
Steps
Data
Original data was excel peak-valley TH w/data points in domain
nCode
Scaled TH to 24 kN, padded beginning and end of file with zeros
Up-sampled files @ 20.48 Hz (Interpolated, Half-sine) so they could be iterated in RPC
Converted TH files to lbf for RPC setup
Inverted data to match polarities of RPC test set up, -lbf=Actuator retract=tension on outboard side of test setup
Exported into RPC Format
In RPC
Used Header mod tool to change sample rate to 204.8 Hz to compress file for 5 Hz test frequency
  Set points per frame and points per group to 1024
  Set up “actuator” channel to correspond with full scales
Used Channel Transformation tool to add displacement for correlation of test data +/- 5”
Modified ramp points at beginning and end of file to reduce ring at start and end of drive (parabola point manipulation)

## Slide 25
Total Fatigue Life: Crack Initiation and Crack Propagation….Whole Life
29 A36 T-Joint Test Results to Date

## Slide 26
Total Fatigue Life: Crack Initiation and Crack Propagation Analysis … Whole Life
October 11, 2017
Comparison - Welded to Machined FEM Stress Distributions
The welded analysis was exactly the same as the machined analysis except the FEM stress distribution input was changed (slightly) from the machined distribution to the welded distribution as shown in the figure on the left…..
And the welding residual stress distribution (shown in the figure on the right) was included in the analysis. No residual stress distribution was input in the machined analysis.

## Slide 27
Total Fatigue Life: Crack Initiation and Crack Propagation Analysis … Whole Life
Whole Life Fatigue Life Predictions to “Failure”
1)The fatigue life predictions of the welded samples appear to be consistent with the fatigue life predictions of the machined samples.
2)All the predicted fatigue lives fall within scatter bands of approximately +/- 2 times the test lives to failure.

## Slide 28
Possibly add welding sequence and measured residual stresses?

## Slide 29
Total Fatigue Life: Crack Initiation and Crack Propagation Analysis… Whole Life
Evaluate Residual Stress Distributions Obtained by Two Different Methods
NIST residual stress distribution may give slightly better correlation to test data
Notes: Welded specimens in groups of 4
Sent specimens out for residual stress measurements to various companies
Understand residual stress effects on actual test lives

## Slide 30: Total Fatigue Life: Crack Initiation and Crack Propagation
Questions?

## Slide 31: Total Fatigue Life: Crack Initiation and Crack Propagation
“We don’t make mistakes, just happy little accidents.” – Bob Ross

## Slide 32: Total Fatigue Life: Crack Initiation and Crack Propagation
Highest Tensile Residual Stress
Side Loaded in Compressive
Specimen Loading
12.1kN, R=0.1 – 7.3 million cycles
Side Loaded in Tensile

## Slide 33: Total Fatigue Life: Crack Initiation and Crack Propagation
APS Residual Stress Distribution,
Surface at ~416 MPa (extrapolated)

## Slide 34: Total Fatigue Life: Crack Initiation and Crack Propagation
Load, Actuator Signal - (N)

## Slide 35: Total Fatigue Life: Crack Initiation and Crack Propagation
Stress induced from load,
Linear Elastic - (MPa)

## Slide 36: Total Fatigue Life: Crack Initiation and Crack Propagation
Residual Stress Offset,
Linear Elastic - (MPa)

## Slide 37: Total Fatigue Life: Crack Initiation and Crack Propagation
Chart: 
| 39 | 37.671107225273666 | 33.774990747593108 | 27.577164466275356 | 19.500000000000004 | 10.09394275899831 | 2.389039487071809E-15 | -10.093942758998313 | -19.499999999999993 | -27.577164466275352 | -33.774990747593108 | -37.671107225273659 | -39
x | 0 | 2.5882 | 5 | 7.0711 | 8.6603 | 9.6593 | 10 | 9.6593 | 8.6603 | 7.0711 | 5 | 2.5882 | 1.2251e-15
Calculated elliptical crack front “to scale” overlaid on fracture surface (P =12.1kN, R=0.1, n=7,000,000 cycles, a=10mm and b=39mm)