## Slide 1
Residual Stress Measurement of a Welded T-Sample using X-ray Diffraction

## Slide 2
ABOUT PROTO
Specializing in X-ray diffraction systems for over 30 years:
  Residual Stress & Retained Austenite Measurement
  Laue Orientation of Single Crystal Materials.
  Powder Diffraction
  X-ray Tubes
  Electropolishers
Customer Base:
  Over 380 XRD systems installed around the world in automotive, aerospace, power generation, marine, military, research & university sectors.
Service Laboratories
  5 service laboratories with 20 XRD systems available for contract measurement work. Fast turn around time, competitive pricing. (USA, Canada, India, China, Poland)

## Slide 4
MORE ABOUT PROTO
Accreditation:
  ISO/IEC 17025:2005 Residual Stress & Retained Austenite Measurement
  ISO/IEC 9000:2015 X-Ray Tube Manufacturing
Major contributors to following Residual Stress specifications:
  ASTM E915
  ASTM E1426
  ASTM E2860
  ASM Handbook Vol. 11
  MFN Shot Peening handbook
  SAE HS-784
Publications:
  Over 80 papers published in peer reviewed journals on residual stress and x-ray diffraction.
Patents:
  Worldwide patents on x-ray diffraction equipment and measurement techniques

## Slide 6
How Best to Achieve the Objective using XRD?
Proposed Approach 1: Measure RS vs. depth to mid-thickness from Side 1 on Sample A, then measure RS vs. depth to mid-thickness from Side 2 on Sample B, then stitch both profiles together for full through thickness RS profiles.
Proposed Approach 2: Measure RS vs. depth to 1/4-thickness from both Side 1 and Side 2 on Sample A only.
Decision: The group opted for Approach 2 due to rarity of remaining samples.

## Slide 7
Measurement Range Selected: RS profiles from the weld toe up to 50 mm away.
Sampled Sides: Both Side 1 and Side 2.
Directions Sampled: Measure RS both perpendicular and parallel to the weld.
Depths: RS measured from the surface up to ¼ thickness.
Why do the above?: To capture both surface and subsurface RS gradients known to typically exist in weldments.

## Slide 8
All of the Data – there was a mountain of it collected

## Slide 9
Limited Data Sets for Ease of Review – Perpendicular RS only

## Slide 10
Note: Welds are never perfect neither along the length nor side to side.

## Slide 11
1 mm

## Slide 12
If modeling actually worked for predicting RS, we would not need measurements anymore!

## Slide 13
1 mm

## Slide 14
Neutron and Synchrotron need a very accurate d0 – the problem is d0 is not a constant through the HAZ and weld metal – i.e. not suitable for measuring such welds. So we are left with XRD and Contour which are insensitive to small changes in d0.

## Slide 15
0 mm

## Slide 16
1 mm

## Slide 17
2 mm

## Slide 18
3 mm

## Slide 19
4 mm

## Slide 20
5 mm

## Slide 21
8 mm

## Slide 22
11 mm

## Slide 23
21 mm

## Slide 24
39 mm

## Slide 25
8 mm

## Slide 26
Improvements Required
Modeling needs some work – does not accurately predict RS in welds.
With better estimates of d0 through the changes in microstructure in the weld HAZ, Neutron and Synchrotron data could be corrected/improved – currently they do not appear suitable for characterizing welds.
Cold working effects on Blanchard ground plates obfuscate welding effects i.e. surface XRD alone is insufficient.
Contour method does not capture near surface cold working very well.
Welds are rarely physically perfect – this must be taken into account during experiment design.

## Slide 27
Conclusions
XRD was successful in capturing RS data in Welded T-Sample 6-2.
Large surface and subsurface RS gradients are present in the welds.
XRD and Contour methods are insensitive to changes in d0 and as such work well for measuring RS in welds.
Surface and near surface RS can play a significant role in crack initiation so remains important.
Subsurface RS is important for damage tolerance and crack propagation.
XRD can be used to measure multiple directions in the same sample.

## Slide 28
Additional Slides

## Slide 29
Soft x-rays constructively interfere with the crystals in the material
The diffraction “cone” angle “q” varies with change in “d” to strain as per Bragg’s Law: nl=2d sin q

## Slide 30: Elasticity - Hooke’s Law
Elasticity
Hooke’s law (1D):
E: Young’s modulus
The loading is reversible
Hooke’s law (3D) :
dij=0 if i≠ j, dij=1 if i= j
Stress – Strain curve

## Slide 31
Conventional XRD vs. Synchrotron EDXRD

## Slide 32
EVEN MORE STILL ABOUT PROTO Product Overview
Portable RS and RA
iXRD
iXRD Combo
iXRD Modular Mapping
iXRD Gantry
Ultraportable RS
mXRD Hand Placed
Laboratory RS and RA
LXRD
LXRD Widebody
LXRD Microarea
LXRD Modular Mapping
LXRD Gantry
Powder Diffraction
AXRD Benchtop
Single Crystal Orientation
LAUE HT
LAUE COS
X-ray Tubes
XRT 60
XRT 30
XRT 16
X-ray Tube Power Supplies
iXPS 300
iXPS 3000
Sample Prep
8818-V3 Electropolisher
Electrolyte “A”
Software
XRDWIN 2.0
XRDWIN Powder
XRDWIN Laue
Specialty RS
iXRD Bolthole
mXRD EPRI
MG15
Accessories
4-point bend RA & RS reference standards