## Slide 1
Presented By
Nilesh Gaonkar
October, 23 2019
Validation of a computational model for predicting fatigue life

## Slide 2
Background and Motivation
Fatigue stress?
Probability distribution function for fatigue life for stress for a given number of load cycles to failure shown in yellow and for number of load cycles to failure for a given stress shown in blue.
Each gray circle shows fatigue life for one fatigue test plotted in the space of the number of load cycles to failure vs. stress in sample space.

## Slide 3
Problem Statement - SAE FDE Project
Why T-Joint Specimen?
Most large structures are often subjected to bending loads.
Typically, in a fatigue problem in a welded structure the crack initiates at the weld toe.
Ease in test setup and fixturing.
Why A36 steel?
Commonly used in ground vehicle industry
Low strength, high ductility

## Slide 4: SAE Fatigue Design & Evaluation Project
Real World Engineering Design Problems
SAE FD&E “T-Bar” Test/Analysis Effort
Legend:
High Confidence Inputs/Analysis!
Define Improved Practice?

## Slide 5
Problem Statement - SAE FDE Project
MTS FlexTest IIm Controller
– Load Control
– Running tests at 5.1 Hz
MTS 793 Series Software
– Basic Testware (constant amplitude)
– MultiPurpose Testware (block loading)
– RPC Pro (variable amplitude loading TBS)
MTS 244 Series Hydraulic Actuator
  – 11 Kip (50 kN) x 6” (152 mm) stroke
– 252.25 Series dual stage servo valve
– MTS Load cell and LVDT
SOMAT eDAQ Lite
– Record time history file
– Collecting Load & Displacement
– Collect strain on certain specimens
Dino-Lite USB Cameras / Laptop
– Capture time-lapse video at weld toe
SAE Test Set Up
Load cell
Light to
Facilitate
videos
Test
Article
Stiff back and
actuator

## Slide 6
Problem Statement - SAE FDE Project
Overall applied load line measured from the center axis of the actuator rod to the toe radius was 222.25mm
The testing was performed using three forms of loading time histories:
  Constant amplitude loading
  Block cycle loading, and
  Variable amplitude loading.
Test run at frequency of 5.1Hz in load control until failure.
The different forms of loadings were selected to generate a range of fatigue lives (10,000 to 1,000,000 cycles) using various load range and mean load level sequences.
Loading Histories

## Slide 7: Problem Statement - SAE FDE Project
Constant Amplitude Loading:
Multiple Initiation Locations Grow Into One Main Crack
24 kN, R= 0.1
24 kN, R= 0.3
24 kN, R= 0.3
18 kN, R= 0.1
14 kN, R= 0.1

## Slide 8: Problem Statement - SAE FDE Project
Marker Bands
(Striations or beach marks)
Block Loading
The block cycle sequence was assembled to run two different loading blocks alternating between 5,000 cycles at 24kN, R=0.1 and 40,000 cycles at 24kN, R=0.5, one sequence right after the other.
Marker bands progress through the fracture surface indicating the two different load levels and R ratios used in the time history

## Slide 9
Problem statement - SAE FDE Project
Case | Max Load (kN) | R Ratio Dimensionless | Experimental Test Cycles
Case 1 | 24 | 0.1 | 58,481
 | 24 | 0.1 | 70,011
Case 2 | 24** | 0.3 | 266,012
 | 24 | 0.3 | 218,671
 | 24 | 0.3 | 200,464
Case 3 | 24* | 0.5 | 2,471,943
Case 4 | 18*** | 0.1 | 424,431
 | 18 | 0.1 | 411,745
Case 5 | 14* | 0.1 | 3,495,011
Case 6 | 24 | ****Block Load: 0.1/0.5 | 326,135
 | 24 | ****Block Load: 0.1/0.5 | 301,938
Note |  |  | 
*Run-out |  |  | 
**Tested after R=0.5 run-out |  |  | 
***Tested after R=0.1 run-out |  |  | 
****5k 24kN R=0.1 Cycles followed by 40k 24kN R=0.5 Cycles |  |  | 

## Slide 10
Methodology
Comparison of simulated through thickness YY-Max Stress distribution for different mesh

## Slide 11: Methodology
Comparing the simulated through thickness
Min-Max YY-Stress distribution
Case 1: 24 KN, R = 0.1 (Max load 24 KN, Min load 2.4 KN)
Case 2: 24 KN, R = 0.3 (Max load 24 KN, Min load 7.2 KN)
Case 3: 24 KN, R = 0.5 (Max load 24 KN, Min load 12 KN)

## Slide 12: Result and Discussion
Case 1 - Load 24KN, R 0.1: Predicted YY-Stress plot of a Gauss Point near crack nucleation region.
Gauss Point
Crack Nucleation

## Slide 13: Result and Discussion
Predicted YY-Stress plot for one gauss point near crack tip region for which damage
value reach 1.0 at time step 60, crack length=0.646mm, fatigue cycles 59,077
Gauss Point
Crack Tip

## Slide 14: Result and Discussion
Predicted Ramberg-Osgood Hysteresis loop for one Gauss Point
24 KN, R = 0.1
24 KN, R = 0.3
24 KN, R = 0.5
59,077
Load cycles to failure
566,025
Load cycles to failure
8,556,150
Load cycles to failure

## Slide 15: Result and Discussion
Comparing predicted fatigue crack length vs time step
57,663 Cycles
543,895 Cycles
8,219,600 Cycles
59,114 Cycles
565,985 Cycles
8,556,200 Cycles
Case 1: 24 KN, R 0.1
Case 2: 24 KN, R 0.3
Case 3: 24 KN, R 0.5

## Slide 16: Result and Discussion
VrSuite Fatigue Model - Displacement and Damage View
Case 1: 24 KN, R = 0.1
Crack Length = 18.786mm
59,114 load cycles

## Slide 17: Result and Discussion
VrSuite Computational Fatigue Model – Crack growth
Case 1: 24 KN, R = 0.1
Crack Length = 18.786 mm
59,114 load cycles

## Slide 18: Result and Discussion
VrSuite Computational Fatigue Model – Crack growth
Case 2: 24 KN, R = 0.3
Crack Length = 3.463mm
565,985 load cycles
Case 3: 24 KN, R = 0.5
Crack Length = 2.795mm
8,556,200 load cycles

## Slide 19: Result and Discussion
Variable amplitude – Block loading history
Block 1: 24KN, R 0.1, 5000 cycles
Block 2: 24KN, R 0.5, 40,000 cycles
Predicted YY-Stress distribution for one Gauss point for which damage value reaches 1.0
540,370 Cycles

## Slide 20: Result and Discussion
Block Loading - Hysteresis loop for one Gauss Point
Block 1 : 24KN, R 0.1, 5000 cycles, Block 2: 24KN, R 0.5, 40,000 cycles

## Slide 21: Result and Discussion
Block Loading - Predicted Fatigue crack length vs No of cycles

## Slide 22: Result and Discussion
Case | Max Load (kN) | R Ratio Dimensionless | Experimental Test Cycles | Mesh | Predicted Fatigue Cycles to Failure
Case 1 | 24 | 0.1 | 58,481 | Mesh III | 60,428
 | 24 | 0.1 | 70,011 |  | 
Case 2 | 24** | 0.3 | 266,012 | Mesh II | 402,772
 | 24 | 0.3 | 218,671 |  | 
 | 24 | 0.3 | 200,464 |  | 
Case 3 | 24* | 0.5 | 2,471,943 | Mesh II | 3,420,890
Case 4 | 18*** | 0.1 | 424,431 | Mesh II | 407,016
 | 18 | 0.1 | 411,745 |  | 
Case 5 | 14* | 0.1 | 3,495,011 | Mesh II | 7,187,780
Case 6 | 24 | ****Block Load: 0.1/0.5 | 326,135 | Mesh II | 540,387
 | 24 | ****Block Load: 0.1/0.5 | 301,938 |  | 
Note: *Run-out **Tested after R=0.5 run-out ***Tested after R=0.1 run-out ****5k 24kN R=0.1 Cycles followed by 40k 24kN R=0.5 Cycles |  |  |  |  | 

## Slide 23: Result and Discussion
Case 5: 14 KN R 0.1
Gauss point Stress distribution at Time Step 1
Crack growth

## Slide 24: Result and Discussion
Case 5: 14 KN R 0.1
Gauss point Stress and Strain distribution at Time Step 60 for 14 KN R 0.1

## Slide 25: Result and Discussion
Case 1: 24 KN R 0.1 Crack Growth

## Slide 26: Microstructure Phases of A36 alloy
SEM measurements
Pearlite
Ferrite
With C | Weight% | Atomic%
C K | 15.47 | 45.92
Si K | 0.18 | 0.23
Cr K | 0.15 | 0.10
Mn K | 0.75 | 0.49
Fe K | 83.10 | 53.06
Cu K | 0.35 | 0.20
Totals | 100.00 | 
Without C | Weight% | Atomic%
Si K | 0.23 | 0.46
Cr K | 0.17 | 0.19
Mn K | 0.89 | 0.91
Fe K | 98.28 | 98.08
Cu K | 0.42 | 0.37
Totals | 100.00 | 
With C | Weight% | Atomic%
C K | 12.21 | 39.19
Si K | 0.26 | 0.36
Cr K | 0.22 | 0.16
Mn K | 0.62 | 0.44
Fe K | 86.40 | 59.67
Cu K | 0.29 | 0.18
Totals | 100.00 | 
Without C | Weight% | Atomic%
Si K | 0.33 | 0.65
Cr K | 0.25 | 0.26
Mn K | 0.71 | 0.72
Fe K | 98.38 | 98.08
Cu K | 0.34 | 0.30
Totals | 100.00 | 
Ferrite and EDS composition

## Slide 27: The overall composition (including both ferrite and pearlite)
Ferrite + Pearlite
Element | Weight% | Atomic%
Si K | 0.32 | 0.63
Cr K | 0.09 | 0.10
Mn K | 0.63 | 0.64
Fe K | 98.71 | 98.41
Cu K | 0.25 | 0.22
Totals | 100.00 | 

## Slide 28: The welds
The welds are made of a steel with slightly higher Mn and Si content than the base alloys A36
Element | Weight% | Atomic%
Si K | 0.67 | 1.33
Mn K | 1.28 | 1.29
Fe K | 98.05 | 97.39
Totals | 100.00 | 

## Slide 29: Residual Stress Prediction

## Slide 30
Chart: 
| 0 | 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9 | 0.95 | 1
 | 263732000 | 210581000 | 145051000 | 77684400 | 71477900 | 47922700 | 17778900 | 27936000 | -12865700 | 493551 | 20845900 | 45267400 | 32098900 | 45585600 | 28863800 | 46502500 | 76663600 | 86800700 | 213389000 | 256003000 | 119272000
Goldak Technologies Inc.

## Slide 31
    Analyze fatigue life of welded structures.
    Compare experimental force displacement vs Virtual force displacement as a function of load cycles.
    Issues that are not well understood:
      Role of residual stress in fatigue life.
      Role of compressive hydrostatic stress in fatigue life, e.g. R = -1.0
      Role of cyclic loading in relaxing residual stress.
Future Work