## Slide 1: SAE FD&E Residual Stress Committee
Fall 2019 Update
Casey Gales

## Slide 2: A36 Monotonic Stress-Strain Data
 |  |  | Calculated Properties |  |  |  |  | 
ID | Area Original (Ao) (mm^2) | Ultimate Load (N) | Ultimate Stress (MPa) | Yield Strength (MPa) | Young's Modulus (MPa) | Elongation, ∆L (mm) | Elongation (%) | Area Reduction (%)
F1 | 74.82 | 37205 | 497 | 271.4 | 205574 |  |  | 
F2 | 74.58 | 37143 | 498 | 273.6 | 196845 |  |  | 
F3 | 74.94 | 36726 | 490 | 264.7 | 206820 |  |  | 
F4 | 74.64 |  |  |  |  |  |  | 
F5 | 74.88 |  |  |  |  |  |  | 
F6 | 74.70 |  |  |  |  |  |  | 
R1 | 31.72 | 15602 | 492 | 254.3 | 203435 |  |  | 
R2 | 31.71 | 15688 | 495 | 264.7 | 203608 |  |  | 
R3 | 31.53 | 15499 | 492 | 303.8 | 208092 |  |  | 
R4 |  |  |  |  |  |  |  | 
R5 |  |  |  |  |  |  |  | 
R6 |  |  |  |  |  |  |  | 
Tested ASTM E8 and ASTM E606
Results to be posted on website
3 samples of each are still available
Compact Crack Growth Specimen’s are planned by Dan L.

## Slide 3: Microscopy and Micro CT
Sent a section of weld to Dr. Goldak (and team)
Will perform microscopy of the HAZ
  Assist with residual stress analysis
Potentially will perform micro CT of weld
  Looking for funding
  Looking for alternative sources

## Slide 4: Correlation of Measurement vs Predicted Residual Stress
Improvement to the measured data
  Corrected for D0 changes through thickness
ProtoXRD provided D0 vs thickness
  Hauk’s Method
  D-Perpendicular
  3rd method in process

## Slide 5: Future Work
Correct measured residual stresses with D0 versus depth data
  Work with Thomas G. from NIST for Neutron Data
  Work with Justin/APS for EDD data
Dr. Goldak [and team] to provide updated residual stress prediction
Fatigue testing samples with modified residual stress
  Relieved and Compressive
  Predictive work to support testing- Dan L.